# 6721R	RESENE PAINTING INTERIOR

## 1.	GENERAL

If you have pre-customised this work section using the "questions and answers" provided as part of the downloading process, it may be necessary to amend some clauses to suit the final project-specific version.

The section must still be checked and customised to suit the project being specified, by removing any other irrelevant details and adding project-specific details and selections.

This section relates to the surface preparation, painting and clear finishing of new and existing interior substrates using Resene architectural and decorative coating systems.

Modify or extend the above description to suit the project being specified.

This 6721R RESENE PAINTING INTERIOR section is intended to be combined as appropriate with the sections listed below and they collectively comprise painting work:

-	6700R RESENE PAINTING GENERAL

-	6711R RESENE PAINTING EXTERIOR

-	6711RE RESENE ENVIRONMENTAL PAINTING EXTERIOR

These sections have been written for use with Resene Surface Information & Preparation Data Sheets (SIPDS) and Resene's online product Technical Data Sheets.  Modify and extend the selected systems (refer to SELECTIONS) as necessary for the substrate and its particular location (e.g. the substrate may be the same for bathroom and bedroom but the finish may differ).

Add project-specific clauses where extensive masking and spraying of coatings is involved; especially where solventborne products are specified.  Add clauses when specifying spray or roller-applied high-build products, or when specifying heavy-duty and solid vinyl wallcoverings.

For specific technical information call the Resene Technical Helpline 0800 RESENE (0800 737 363) or at www.resene.co.nz

Refer to the Resene One-Line specifications and product data manual for a comprehensive listing of Resene One-Line specification systems. Include the Resene One-Line specifications in any finishes/colour schemes prepared for the project.

Related work

### 1.1	RELATED WORK

Refer to 6700R RESENE PAINTING GENERAL for general matters related to painting work.

Refer to 6711R RESENE PAINTING EXTERIOR for exterior paint systems.

Refer to 6711RE RESENE ENVIRONMENTAL PAINTING EXTERIOR for exterior paint systems.

Modify or delete, include cross references to other sections where these contain related work.

Other related sections in Masterspec Standard could be 6745R RESENE PROTECTIVE COATINGS - STEELWORK for protective coatings.

Requirements

### 1.2	SAMPLES

Refer to the general section 1270 CONSTRUCTION for details of how samples will be reviewed and how instructions to proceed will be given. Provide the following samples for review:

|  | Sample A | Sample B | Sample C |
| --- | --- | --- | --- |
| Sample description: | ~ | ~ | ~ |
| Sample type: | ~ | ~ | ~ |
| Number: | ~ | ~ | ~ |
| Location: | ~ | ~ | ~ |
| Supporting documentation: | ~ | ~ | ~ |
| Reviewer: | Contract administrator ~ | Contract administrator ~ | Contract administrator ~ |
| Time for review: | 10 working days ~ | 10 working days ~ | 10 working days ~ |
| Review criteria: | ~ | ~ | ~ |

The intention of this clause is to allow samples to be obtained that are not otherwise readily available to a reviewer.

Delete rows and columns not required or add "n/a".

| Sample description: | Describe the sample, size etc. Prepare samples of the finished work as scheduled, including preparation and colour as specified. |
| --- | --- |
| Sample type: | Portable sample for review Portable control sample Fixed sample for review Fixed control sample Control samples define requirements for type and quality and are used for comparison purposes throughout the contract. A "portable" sample is a sample that is easily movable, convenient for carrying. A "fixed" sample is a sample (semi) permanently placed. Expand on these terms as necessary. |
| Number: | State number of samples required, e.g. a minimum of three control samples - portable allow a sample to be retained on site with the other samples retained by the contract administrator and contractor. |
| Location: | Identify location of fixed samples, e.g. off site, on site, in situ |
| Supporting documentation: | Describe any additional documents required to support the review. |
| Reviewer: | Modify to suit the project, add additional reviewers if required |
| Time for review: | Alter time if required. Expand to state timing in relation to when and where the sample is provided, e.g. at first site meeting. |
| Review criteria: | For example: - Appearance - Texture - Colour Add any critical items. Provide clarity for work that is not dependent on the review to continue. |

## 2.	PRODUCTS

Materials

### 2.1	PAINT TYPES GENERALLY/ THINNERS AND ADDITIVES

Refer to 6700R RESENE PAINTING GENERAL for product clauses.

Modify or extend, including adding clauses to this section where product information relates exclusively to interior painting.

## 3.	EXECUTION

Conditions

### 3.1	EXECUTION

Refer to 6700R RESENE PAINTING GENERAL for execution clauses.

Modify or extend, including adding clauses to this section where product information relates exclusively to interior painting.

## 4.	SELECTIONS

Substitutions are not permitted to the following, unless stated otherwise.

### 4.1	INSPECTION OF WORK

| Stage | Resene SIPDS number/system |
| --- | --- |
| ~ | ~ |

The level of inspection will depend on the nature of the project and will range from full for large or complex projects, through to intermittent for straightforward work to occasional for initially establishing the standards of execution.  Refer to AS/NZS 2311 Appendix C, Inspection and Testing, for more background.

### 4.2	BACK PAINTING SCHEDULE

Paint 2 coats (including any pre-prime) usually to match exposed face coating.  If there is no coating use water resistant clear finish sealer.

Lining type	Extent of back painting

~	~

Amend to suit project requirements

Extent options:	To lining manufacturer's requirements

Bottom edge & 150mm up

Paint whole back, bottom & concealed edges of lining

Paint lining under trim before fixing

Paint whole back, bottom & concealed edges of trim

Note;

In most cases only a requirement of wet/damp area linings.

Some pre-finished lining may still need backpainting in wet areas.

Paint, stain and clear finishes can have different sorts of requirements.

Some tiled substrates are recommended to have the whole back painted/sealed.

### 4.3	HARDWARE

Hardware for removal:	~

Paint system schedules

These suggested schedules may be included here.  However they may also be part of a finishes schedule located elsewhere in the specification, may be included on the drawings, or even documented separately.

### 4.4	INTERIOR FINISHES

| Room name | Ref | Substrate | RESENE Spec Number | Colour |
| --- | --- | --- | --- | --- |
| Living | G02 | Ceiling-Plasterboard | ~ |  |
|  |  | Exposed Rafters | ~ |  |
|  |  | Walls - Plasterboard | ~ |  |
|  |  | Trim - Timber | ~ |  |
|  |  | Doors - Paint Finish | ~ |  |
| Dining | G03 | Ceiling - Plasterboard | ~ |  |
|  |  | Exposed Rafters | ~ |  |
|  |  | Walls - Plasterboard | ~ |  |
|  |  | Timber Panelling | ~ |  |
|  |  | Trim - Timber | ~ |  |
|  |  | Doors - Paint Finish | ~ |  |

Dark colours may cause warping on unstable substrates.

Resene interior paint systems

INTERIOR PAINT SYSTEMS: Supply the listed Resene systems for the following substrates.

Note: Select the appropriate first coat by deleting those not applicable.

For a current list of VOCs for Resene products see

www.resene.co.nz/archspec/datashts/vocsummary.pdf.

For information on how to earn Green Star NZ points with paint see

www.resene.co.nz/greenstarnz.htm.

For a current list of Resene Environmental Choice NZ approved paints see

www.resene.co.nz/comn/envissue/paintlst.htm

Systems which provide an option for all Environmental Choice (EC) products to be selected are noted with (EC) after the One-Line Spec Reference.  If the clause contains product options which are not EC approved these are noted with NEC after the product.  These must be deleted to specify a fully compliant EC system

Plasterboard - new

### 4.5	RESENE NEW INTERIOR PLASTERBOARD, WALLS - DRY AREAS (LEVEL 4 FINISH)

Surface Prep:	Resene SIPDS No1 and Spec Sheet 1: 1/1

Fire rating:	Group 1-S. Test Report FH4967

1st coat	Resene Broadwall D403, Waterborne Wallboard Sealer

2nd coat:	Resene Zylone Sheen D302, Waterborne Low Sheen

3rd coat:	Resene Zylone Sheen D302, Waterborne Low Sheen

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Note1: If top coats are changed it may alter the Fire Rating Test Report details.

Note2: Refer to AS/NZS 2589 for guidelines on level of finish. Areas of "Critical Light" require a level 5 finish

For high traffic areas where durable coating is required substitute 2nd & 3rd coats with:

2nd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

3rd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

Where Flat finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

3rd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

### 4.6	RESENE NEW INTERIOR PLASTERBOARD, WALLS - DRY AREAS (LEVEL 5 FINISH)

Surface Prep:	Resene SIPDS No1 and Spec Sheet 1: 1/1

Fire rating:	Group 1-S. Test Report FAR3981

1st coat:	Resene Broadwall Surface Prep & Seal D807, Waterborne Sealer

2nd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

3rd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Note1: If top coats are changed it may alter the Fire Rating Test Report details.

Note2: Refer to AS/NZS 2589 for guidelines on level of finish.

For Critical Light areas or where a Flat finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

3rd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

### 4.7	RESENE NEW INTERIOR PLASTERBOARD, WALLS - WET AREAS

Surface Prep:	Resene SIPDS No1 and Spec Sheet 1A: 1/1

Fire rating:	Group 1-S. Test Report 7-593235-CO

1st coat:	Resene Sureseal D42, solvent-borne Pigmented Sealer (NEC)

2nd coat:	Resene SpaceCote Low Sheen Kitchen & Bathroom D311K Waterborne Enamel

3rd coat:	Resene SpaceCote Low Sheen Kitchen & Bathroom D311K Waterborne Enamel

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Note: If top coats are changed it may alter the Fire Rating Test Report details.

Where Flat finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene SpaceCote Flat Kitchen & Bathroom D314K Waterborne Enamel

3rd coat:	Resene SpaceCote Flat Kitchen & Bathroom D314K Waterborne Enamel

Where Semi-Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Lustacryl Kitchen & Bathroom D310K Waterborne Enamel

3rd coat:	Resene Lustacryl Kitchen & Bathroom D310K Waterborne Enamel

### 4.8	RESENE NEW INTERIOR PLASTERBOARD, WALLS - CLINICAL DRY AREAS

Surface Prep:	Resene SIPDS No1 and Spec Sheet 1: 1/1

Fire rating:	Group 1-S, Test Report FH4925

1st coat:	Resene Broadwall D403, Waterborne Wallboard Sealer

2nd coat:	Resene ClinicalCote Satin D318, Waterborne

3rd coat:	Resene ClinicalCote Satin D318, Waterborne

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Note: If top coats are changed it may alter the Fire Rating Test Report details.

Where Low Sheen finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene ClinicalCote Low Sheen D318, Waterborne

3rd coat:	Resene ClinicalCote Low Sheen D318, Waterborne

For Clinical Walls Wet Areas refer to standard RESENE NEW INTERIOR PLASTERBOARD, WALLS, WET AREAS clause.

### 4.9	RESENE NEW INTERIOR PLASTERBOARD, CEILINGS - DRY AREAS (LEVEL 4 FINISH)

Surface Prep:	Resene SIPDS No1 and Spec Sheet 1: 1/1

Fire rating:	Group 1-S, Test Report FH4967

1st coat:	Resene Broadwall D403, Waterborne Wallboard Sealer

2nd coat:	Resene Ceiling Paint D305, Waterborne Flat

3rd coat:	Resene Ceiling Paint D305, Waterborne Flat

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Note1: If top coats are changed it may alter the Fire Rating Test Report details.

Note 2: Refer to AS/NZS 2589 for guidelines on level of finish. Areas of “Critical Light” require a Level 5 finish

Where durable easily cleaned coating is required substitute 2nd & 3rd coats with:

2nd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

3rd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

### 4.10	RESENE NEW INTERIOR PLASTERBOARD, CEILINGS - DRY AREAS (LEVEL 5 FINISH)

Surface Prep:	Resene SIPDS No1 and Spec Sheet 1: 1/1

Fire rating:	Group 1-S, Test Report FAR3981

1st coat:	Resene Broadwall Surface Prep & Seal D807, Waterborne Sealer

2nd coat:	Resene Ceiling Paint D305, Waterborne Flat

3rd coat:	Resene Ceiling Paint D305, Waterborne Flat

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Note 1: If top coats are changed it may alter the Fire Rating Test Report details.

Note 2: Refer to AS/NZS 2589 for guidelines on level of finish.

Where durable easily cleaned coating is required substitute 2nd & 3rd coats with:

2nd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

3rd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

### 4.11	RESENE NEW INTERIOR PLASTERBOARD, CEILINGS - WET AREAS

Surface Prep:	Resene SIPDS No1 and Spec Sheet 1A: 1/1

Fire rating:	Group 1-S, Test Report 7-593235-CO

1st coat:	Resene Sureseal D42, solvent-borne Pigmented Sealer (NEC)

2nd coat:	Resene SpaceCote Flat Kitchen & Bathroom D314K, Waterborne Enamel

3rd coat:	Resene SpaceCote Flat Kitchen & Bathroom D314K, Waterborne Enamel

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Note: If top coats are changed it may alter the Fire Rating Test Report details.

Where Low Sheen finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene SpaceCote Low Sheen Kitchen & Bathroom D311K, Waterborne Enamel

3rd coat:	Resene SpaceCote Low Sheen Kitchen & Bathroom D311K, Waterborne Enamel

Where Semi-Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Lustacryl Kitchen & Bathroom D310K, Waterborne Enamel

3rd coat:	Resene Lustacryl Kitchen & Bathroom D310K, Waterborne Enamel

### 4.12	RESENE NEW INTERIOR PLASTERBOARD, CEILINGS - CLINICAL DRY AREAS

Surface Prep:	Resene SIPDS No1 and Spec Sheet 1: 1/1

Fire rating:	Group 1-S, Test Report FH4925

1st coat:	Resene Broadwall D403, Waterborne Wallboard Sealer

2nd coat:	Resene ClinicalCote Low Sheen D318, Waterborne

3rd coat:	Resene ClinicalCote Low Sheen D318, Waterborne

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Flat finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

3rd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

Where Satin finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene ClinicalCote Satin D318, Waterborne

3rd coat:	Resene ClinicalCote Satin D318, Waterborne

For Clinical Ceilings Wet Areas refer to standard RESENE NEW INTERIOR PLASTERBOARD, CEILINGS, WET AREAS clause.

Plasterboard - existing

### 4.13	RESENE EXISTING INTERIOR PLASTERBOARD, WALLS - DRY AREAS

Surface Prep:	Resene SIPDS No1 and Spec Sheet 1: 1/3

Spot Prime:	Resene Broadwall D403, Waterborne Wallboard Sealer

1st coat:	Resene Zylone Sheen D302, Waterborne Low Sheen

2nd coat:	Resene Zylone Sheen D302, Waterborne Low Sheen

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

For high traffic areas where durable coating is required substitute 1st & 2nd coats with:

1st coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

2nd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

Where Flat finish is required substitute 1st & 2nd coats with:

1st coat:	Resene SpaceCote Flat D314, Waterborne Enamel

2nd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

### 4.14	RESENE EXISTING INTERIOR PLASTERBOARD, WALLS - WET AREAS

Surface Prep:	Resene SIPDS No1 and Spec Sheet 1A: 1/3

Spot Prime:	Resene Sureseal D42, solvent-borne Pigmented Sealer (NEC)

1st coat:	Resene SpaceCote Low Sheen Kitchen & Bathroom D311K, Waterborne Enamel

2nd coat:	Resene SpaceCote Low Sheen Kitchen & Bathroom D311K, Waterborne Enamel

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Flat finish is required substitute 1st & 2nd coats with:

1st coat:	Resene SpaceCote Flat Kitchen & Bathroom D314K, Waterborne Enamel

2nd coat:	Resene SpaceCote Flat Kitchen & Bathroom D314K, Waterborne Enamel

Where Semi-Gloss finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Lustacryl Kitchen & Bathroom D310K, Waterborne Enamel

2nd coat:	Resene Lustacryl Kitchen & Bathroom D310K, Waterborne Enamel

Where solvent-borne Low Sheen finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Room Velvet D320, solvent-borne Enamel

2nd coat:	Resene Room Velvet D320, solvent-borne Enamel

### 4.15	RESENE EXISTING INTERIOR PLASTERBOARD, WALLS - CLINICAL DRY AREAS

Surface Prep:	Resene SIPDS No1 and Spec Sheet 1: 1/3

Spot Prime:	Resene Broadwall D403, Waterborne Wallboard Sealer

1st coat:	Resene ClinicalCote Satin D318, Waterborne

2nd coat:	Resene ClinicalCote Satin D318, Waterborne

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Low Sheen finish is required substitute 1st & 2nd coats with:

1st coat:	Resene ClinicalCote Low Sheen D318, Waterborne

2nd coat:	Resene ClinicalCote Low Sheen D318, Waterborne

For Clinical Walls Wet Areas refer to standard RESENE EXISTING INTERIOR PLASTERBOARD, WALLS, WET AREAS clause.

### 4.16	RESENE EXISTING INTERIOR PLASTERBOARD, CEILINGS - DRY AREAS

Surface Prep:	Resene SIPDS No1 and Spec Sheet 1: 1/3

Spot Prime:	Resene Broadwall D403, Waterborne Wallboard Sealer

1st coat:	Resene Ceiling Paint D305, Waterborne Flat

2nd coat:	Resene Ceiling Paint D305, Waterborne Flat

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where durable easily cleaned coating is required substitute 1st & 2nd coats with:

1st coat:	Resene SpaceCote Flat D314, Waterborne Enamel

2nd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

### 4.17	RESENE EXISTING INTERIOR PLASTERBOARD, CEILINGS - WET AREAS

Surface Prep:	Resene SIPDS No1 and Spec Sheet 1A: 1/3

Spot Prime:	Resene Sureseal D42, solvent-borne Pigmented Sealer (NEC)

1st coat:	Resene SpaceCote Flat Kitchen & Bathroom D314K, Waterborne Enamel

2nd coat:	Resene SpaceCote Flat Kitchen & Bathroom D314K, Waterborne Enamel

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Low Sheen finish is required substitute 1st & 2nd coats with:

1st coat:	Resene SpaceCote Low Sheen Kitchen & Bathroom D311K, Waterborne Enamel

2nd coat:	Resene SpaceCote Low Sheen Kitchen & Bathroom D311K, Waterborne Enamel

Where Semi-Gloss finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Lustacryl Kitchen & Bathroom D310K, Waterborne Enamel

2nd coat:	Resene Lustacryl Kitchen & Bathroom D310K, Waterborne Enamel

Where solvent-borne Low Sheen finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Room Velvet D320, solvent-borne Enamel

2nd coat:	Resene Room Velvet D320, solvent-borne Enamel

### 4.18	RESENE EXISTING INTERIOR PLASTERBOARD, CEILINGS - CLINICAL DRY AREAS

Surface Prep:	Resene SIPDS No1 and Spec Sheet 1: 1/3

Spot Prime:	Resene Broadwall D403, Waterborne Wallboard Sealer

1st coat:	Resene ClinicalCote Low Sheen D318, Waterborne

2nd coat:	Resene ClinicalCote Low Sheen D318, Waterborne

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Flat finish is required substitute 1st & 2nd coats with:

1st coat:	Resene SpaceCote Flat D314, Waterborne Enamel

2nd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

Where Satin finish is required substitute 1st & 2nd coats with:

1st coat:	Resene ClinicalCote Satin D318, Waterborne

2nd coat:	Resene ClinicalCote Satin D318, Waterborne

For Clinical Ceilings Wet Areas refer to standard RESENE EXISTING INTERIOR PLASTERBOARD, CEILINGS, WET AREAS clause

Interior timber - new

### 4.19	RESENE AQUALAQ: TIMBER JOINERY, MDF, CABINETRY – WATERBORNE LACQUER SOLID COLOUR

Surface Prep:	Resene SIPDS No7 and Spec Sheet 7: 1/1

Note: for use by specialist applicators only

1 to 2 coats:	Resene AquaLAQ Quick Dry Sealer - interior waterborne

2 to 3 coats:	Resene AquaLAQ Colour Coat - interior waterborne satin

Note: Contact help@reseneauto.co.nz for Specialist applicator details and information

### 4.20	RESENE AQUALAQ: TIMBER JOINERY, MDF, CABINETRY – WATERBORNE LACQUER SOLID COLOUR & CLEAR COAT SATIN

Surface Prep:	Resene SIPDS No7 and Spec Sheet 7: 1/1

Note: for use by specialist applicators only

1 to 2 coats:	Resene AquaLAQ Quick Dry Sealer - interior waterborne

2 to 3 coats:	Resene AquaLAQ Colour Coat - interior waterborne satin

1 to 2 coats:	Resene AquaLAQ Clear Coat - interior waterborne satin

Note: Contact help@reseneauto.co.nz for Specialist applicator details and information

### 4.21	RESENE AQUALAQ TIMBER JOINERY, MDF, CABINETRY – WATERBORNE LACQUER SOLID COLOUR & CLEAR SOFT TOUCH

Surface Prep:	Resene SIPDS No7 and Spec Sheet 7: 1/1

Note: for use by specialist applicators only

1 to 2 coats:	Resene AquaLAQ Quick Dry Sealer - interior waterborne

2 to 3 coats:	Resene AquaLAQ Colour Coat - interior waterborne satin

1 to 2 coats:	Resene AquaLAQ Soft Touch - interior waterborne satin

Note: Contact help@reseneauto.co.nz for Specialist applicator details and information

### 4.22	RESENE AQUALAQ: TIMBER JOINERY, MDF, CABINETRY – WATERBORNE LACQUER SOLID COLOUR & CLEAR COAT MATT

Surface Prep:	Resene SIPDS No7 and Spec Sheet 7: 1/1

Note: for use by specialist applicators only

1 to 2 coats:	Resene AquaLAQ Quick Dry Sealer - interior waterborne

2 to 3 coats:	Resene AquaLAQ Colour Coat - interior waterborne satin

1 to 2 coats:	Resene AquaLAQ Clear Coat - interior waterborne matt

Note: Contact help@reseneauto.co.nz for Specialist applicator details and information

### 4.23	RESENE AQUALAQ: TIMBER JOINERY, MDF, CABINETRY – WATERBORNE LACQUER SOLID COLOUR & CLEAR COAT GLOSS

Surface Prep:	Resene SIPDS No7 and Spec Sheet 7: 1/1

Note: for use by specialist applicators only

1 to 2 coats:	Resene AquaLAQ Quick Dry Sealer - interior waterborne

2 to 3 coats:	Resene AquaLAQ Colour Coat - interior waterborne satin

1 to 2 coats:	Resene AquaLAQ Clear Coat - interior waterborne gloss

Note: Contact help@reseneauto.co.nz for Specialist applicator details and information

### 4.24	RESENE AQUALAQ NEW INTERIOR TIMBER JOINERY, CABINETRY – WATERBORNE LACQUER CLEAR COAT SATIN

Surface Prep:	Resene SIPDS No7 and Spec Sheet 7: 1/1

Note: for use by specialist applicators only

1 to 2 coats:	Resene AquaLAQ Quick Dry Clear Sealer - interior waterborne

2 to 3 coats:	Resene AquaLAQ Clear Coat - interior waterborne satin

Note: Contact help@reseneauto.co.nz for Specialist applicator details and information

### 4.25	RESENE AQUALAQ NEW INTERIOR TIMBER JOINERY, CABINETRY – WATERBORNE LACQUER CLEAR COAT SOFT TOUCH

Surface Prep:	Resene SIPDS No7 and Spec Sheet 7: 1/1

Note: for use by specialist applicators only

1 to 2 coats:	Resene AquaLAQ Quick Dry Clear Sealer - interior waterborne

2 to 3 coats:	Resene AquaLAQ Soft Touch - interior waterborne satin

Note: Contact help@reseneauto.co.nz for Specialist applicator details and information

### 4.26	RESENE AQUALAQ NEW INTERIOR TIMBER JOINERY, CABINETRY – WATERBORNE LACQUER CLEAR COAT MATT

Surface Prep:	Resene SIPDS No7 and Spec Sheet 7: 1/1

Note: for use by specialist applicators only

1 to 2 coats:	Resene AquaLAQ Quick Dry Clear Sealer - interior waterborne

2 to 3 coats:	Resene AquaLAQ Clear Coat - interior waterborne matt

Note: Contact help@reseneauto.co.nz for Specialist applicator details and information

### 4.27	RESENE AQUALAQ NEW INTERIOR TIMBER JOINERY, CABINETRY – WATERBORNE LACQUER CLEAR COAT GLOSS

Surface Prep:	Resene SIPDS No7 and Spec Sheet 7: 1/1

Note: for use by specialist applicators only

1 to 2 coats:	Resene AquaLAQ Quick Dry Clear Sealer - interior waterborne

2 to 3 coats:	Resene AquaLAQ Clear Coat - interior waterborne gloss

Note: Contact help@reseneauto.co.nz for Specialist applicator details and information

### 4.28	RESENE AQUALAQ NEW INTERIOR TIMBER JOINERY, CABINETRY – WATERBORNE STAIN & LACQUER CLEAR COAT SATIN

Surface Prep:	Resene SIPDS No7 and Spec Sheet 7: 1/1

Note: for use by specialist applicators only

1 coat:	Resene Waterborne Colorwood - interior natural wood stain

2 to 3 coats:	Resene AquaLAQ Clear Coat - interior waterborne satin

Note: Contact help@reseneauto.co.nz for Specialist applicator details and information

### 4.29	RESENE AQUALAQ NEW INTERIOR TIMBER JOINERY, CABINETRY – WATERBORNE STAIN & LACQUER CLEAR SOFT TOUCH

Surface Prep:	Resene SIPDS No7 and Spec Sheet 7: 1/1

Note: for use by specialist applicators only

1 coat:	Resene Waterborne Colorwood - interior natural wood stain

2 to 3 coats:	Resene AquaLAQ Soft Touch - interior waterborne satin

Note: Contact help@reseneauto.co.nz for Specialist applicator details and information

### 4.30	RESENE AQUALAQ NEW INTERIOR TIMBER JOINERY, CABINETRY – WATERBORNE STAIN & LACQUER CLEAR COAT MATT

Surface Prep:	Resene SIPDS No7 and Spec Sheet 7: 1/1

Note: for use by specialist applicators only

1 coat:	Resene Waterborne Colorwood - interior natural wood stain

2 to 3 coats:	Resene AquaLAQ Clear Coat - interior waterborne matt

Note: Contact help@reseneauto.co.nz for Specialist applicator details and information

### 4.31	RESENE AQUALAQ NEW INTERIOR TIMBER JOINERY, CABINETRY – WATERBORNE STAIN & LACQUER CLEAR COAT GLOSS

Surface Prep:	Resene SIPDS No7 and Spec Sheet 7: 1/1

Note: for use by specialist applicators only

1 coat:	Resene Waterborne Colorwood - interior natural wood stain

2 to 3 coats:	Resene AquaLAQ Clear Coat - interior waterborne gloss

Note: Contact help@reseneauto.co.nz for Specialist applicator details and information

### 4.32	RESENE NEW INTERIOR TIMBER DOORS, JOINERY, SKIRTING

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 9/1

1st coat:	Resene Quick Dry D45, Waterborne Acrylic Primer Undercoat

2nd coat:	Resene Lustacryl D310, Waterborne Enamel

3rd coat:	Resene Lustacryl D310, Waterborne Enamel

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Enamacryl D309, Waterborne Enamel

3rd coat:	Resene Enamacryl D309, Waterborne Enamel

Where a Low sheen finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene SpaceCote Low sheen D311, Waterborne Enamel

3rd coat:	Resene SpaceCote Low sheen D311, Waterborne Enamel

Where a Semi-Gloss solvent-borne finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Lusta-Glo D33, solvent-borne Semi-Gloss Enamel (NEC)

3rd coat:	Resene Lusta-Glo D33, solvent-borne Semi-Gloss Enamel (NEC)

Where a Low sheen solvent-borne finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Room Velvet D320, solvent-borne Low Sheen Enamel (NEC)

3rd coat:	Resene Room Velvet D320, solvent-borne Low Sheen Enamel (NEC)

### 4.33	RESENE NEW INTERIOR TIMBER DOORS, JOINERY, SKIRTING  - CEDAR

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 9/1

1st coat:	Resene Enamel Undercoat D44, Solvent-borne Undercoat (NEC)

2nd coat:	Resene Lustacryl D310, Waterborne Enamel

3rd coat:	Resene Lustacryl D310, Waterborne Enamel

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Enamacryl D309, Waterborne Enamel

3rd coat:	Resene Enamacryl D309, Waterborne Enamel

Where a Low sheen finish is required substitute 2nd & 3rd coats with:

2nd coat	Resene SpaceCote Low sheen D311, Waterborne Enamel

3rd coat:	Resene SpaceCote Low sheen D311, Waterborne Enamel

Where a Semi-Gloss solvent-borne finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Lusta-Glo D33, solvent-borne Semi-Gloss (NEC)

3rd coat:	Resene Lusta-Glo D33, solvent-borne Semi-Gloss (NEC)

Where a Low sheen solvent-borne finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Room Velvet D320, solvent-borne Low Sheen Enamel (NEC)

3rd coat:	Resene Room Velvet D320, solvent-borne Low Sheen Enamel (NEC)

### 4.34	RESENE NEW INTERIOR TIMBER DOORS, JOINERY, SKIRTING - CLEAR COAT

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 10/1

1st coat:	Resene Aquaclear Satin D59, Waterborne Urethane Varnish

2nd coat:	Resene Aquaclear Satin D59, Waterborne Urethane Varnish

3rd coat:	Resene Aquaclear Satin D59, Waterborne Urethane Varnish

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Gloss finish is required substitute 1st, 2nd & 3rd coats with:

1st coat:	Resene Aquaclear Gloss D59, Waterborne Urethane Varnish

2nd coat:	Resene Aquaclear Gloss D59, Waterborne Urethane Varnish

3rd coat:	Resene Aquaclear Gloss D59, Waterborne Urethane Varnish

Where Semi-Gloss finish is required substitute 1st, 2nd & 3rd coats with:

1st coat:	Resene Aquaclear Semi-Gloss D59, Waterborne Urethane Varnish

2nd coat:	Resene Aquaclear Semi-Gloss D59, Waterborne Urethane Varnish

3rd coat:	Resene Aquaclear Semi-Gloss D59, Waterborne Urethane Varnish

Where Solvent-borne Gloss finish is required substitute 1st, 2nd & 3rd coats with:

1st coat:	Resene Qristal Clear Gloss D52, Solvent-borne Polyurethane Varnish

2nd coat:	Resene Qristal Clear Gloss D52, Solvent-borne Polyurethane Varnish

3rd coat:	Resene Qristal Clear Gloss D52, Solvent-borne Polyurethane Varnish

Where Solvent-borne Semi-Gloss finish is required substitute 1st, 2nd & 3rd coats with:

1st coat:	Resene Qristal Clear Semi-Gloss D52, Solvent-borne Polyurethane

2nd coat:	Resene Qristal Clear Semi-Gloss D52, Solvent-borne Polyurethane

3rd coat:	Resene Qristal Clear Semi-Gloss D52, Solvent-borne Polyurethane

### 4.35	RESENE NEW INTERIOR TIMBER DOORS, JOINERY, SKIRTING - STAIN

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 10/1

1st coat:	Resene Colorwood D50a, Waterborne Natural Wood stain

2nd coat:	Resene Aquaclear Satin D59, Waterborne Urethane Varnish

3rd coat:	Resene Aquaclear Satin D59, Waterborne Urethane Varnish

4th coat:	Resene Aquaclear Satin D59, Waterborne Urethane Varnish

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Gloss finish is required substitute 2nd, 3rd & 4th coats with:

2nd coat:	Resene Aquaclear Gloss D59, Waterborne Urethane Varnish

3rd coat:	Resene Aquaclear Gloss D59, Waterborne Urethane Varnish

4th coat:	Resene Aquaclear Gloss D59, Waterborne Urethane Varnish

Where Semi-Gloss finish is required substitute 2nd, 3rd & 4th coats with:

2nd coat:	Resene Aquaclear Semi-Gloss D59, Waterborne Urethane Varnish

3rd coat:	Resene Aquaclear Semi-Gloss D59, Waterborne Urethane Varnish

4th coat:	Resene Aquaclear Semi-Gloss D59, Waterborne Urethane Varnish

Where Solvent-borne Gloss finish is required substitute 2nd, 3rd & 4th coats with:

2nd coat:	Resene Qristal Clear Gloss D52, Solvent-borne Polyurethane Varnish

3rd coat:	Resene Qristal Clear Gloss D52, Solvent-borne Polyurethane Varnish

4th coat:	Resene Qristal Clear Gloss D52, Solvent-borne Polyurethane Varnish

Where Solvent-borne Semi-Gloss finish is required substitute 2nd, 3rd & 4th coats with:

2nd coat:	Resene Qristal Clear Semi-Gloss D52, Solvent-borne Polyurethane(NEC)

3rd coat:	Resene Qristal Clear Semi-Gloss D52, Solvent-borne Polyurethane(NEC)

4th coat:	Resene Qristal Clear Semi-Gloss D52, Solvent-borne Polyurethane(NEC)

### 4.36	RESENE NEW INTERIOR TIMBER WALLS, CEILINGS - (PARTICLE BOARD, MDF, PLYWOOD)

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 14/1

1st coat:	Resene Quick Dry D45, Waterborne Acrylic Primer Undercoat

2nd coat:	Resene Spacecote Low Sheen D311, Waterborne Enamel

3rd coat:	Resene Spacecote Low Sheen D311, Waterborne Enamel

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a Flat finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

3rd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

Where a Semi-Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Lustacryl D310, Waterborne Enamel

3rd coat:	Resene Lustacryl D310, Waterborne Enamel

Where a standard acrylic finish is required (dry areas only) substitute 2nd & 3rd coats with:

2nd coat:	Resene Zylone Sheen D302, Low Sheen Acrylic

3rd coat:	Resene Zylone Sheen D302, Low Sheen Acrylic

Where a Low Sheen solvent-borne finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Room Velvet D322, Low Sheen solvent-borne Enamel (NEC)

3rd coat:	Resene Room Velvet D322, Low Sheen solvent-borne Enamel (NEC)

Where a Clinical finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene ClinicalCote D318, Semi-Gloss Acrylic

3rd coat:	Resene ClinicalCote D318, Semi-Gloss Acrylic

### 4.37	RESENE NEW INTERIOR TIMBER WALLS, CEILINGS - (PARTICLE BOARD, MDF, PLYWOOD) - CLEAR COAT

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 10/1

1st coat:	Resene Aquaclear Satin D59, Waterborne Urethane Varnish

2nd coat:	Resene Aquaclear Satin D59, Waterborne Urethane Varnish

3rd coat:	Resene Aquaclear Satin D59, Waterborne Urethane Varnish

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Gloss finish is required substitute 1st, 2nd & 3rd coats with:

1st coat:	Resene Aquaclear Gloss D59, Waterborne Urethane Varnish

2nd coat:	Resene Aquaclear Gloss D59, Waterborne Urethane Varnish

3rd coat:	Resene Aquaclear Gloss D59, Waterborne Urethane Varnish

Where Semi-Gloss finish is required substitute 1st, 2nd & 3rd coats with:

1st coat:	Resene Aquaclear Semi-Gloss D59, Waterborne Urethane Varnish

2nd coat:	Resene Aquaclear Semi-Gloss D59, Waterborne Urethane Varnish

3rd coat:	Resene Aquaclear Semi-Gloss D59, Waterborne Urethane Varnish

Where Solvent-borne Gloss finish is required substitute 2nd & 3rd coats only with:

2nd coat:	Resene Qristal Clear Gloss D52, Solvent-borne Polyurethane Varnish

3rd coat:	Resene Qristal Clear Gloss D52, Solvent-borne Polyurethane Varnish

Where Solvent-borne Semi-Gloss finish is required substitute 2nd & 3rd coats only with:

2nd coat:	Resene Qristal Clear Semi-Gloss D52, Solvent-borne Polyurethane(NEC)

3rd coat:	Resene Qristal Clear Semi-Gloss D52, Solvent-borne Polyurethane(NEC)

Where Solvent-borne Flat finish is required substitute 2nd & 3rd coats only with:

2nd coat:	Resene Qristal Clear Flat D52, Solvent-borne Polyurethane Varnish

3rd coat:	Resene Qristal Clear Flat D52, Solvent-borne Polyurethane Varnish

### 4.38	RESENE NEW INTERIOR TIMBER WALLS, CEILINGS - (PARTICLE BOARD, MDF, PLYWOOD) - STAIN

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 10/1

1st coat:	Resene Colorwood D50a, Waterborne Natural Wood stain

2nd coat:	Resene Aquaclear Satin D59, Waterborne Urethane Varnish

3rd coat:	Resene Aquaclear Satin D59, Waterborne Urethane Varnish

4th coat:	Resene Aquaclear Satin D59, Waterborne Urethane Varnish

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Gloss finish is required substitute 2nd, 3rd & 4th coats with:

2nd coat:	Resene Aquaclear Gloss D59, Waterborne Urethane Varnish

3rd coat:	Resene Aquaclear Gloss D59, Waterborne Urethane Varnish

4th coat:	Resene Aquaclear Gloss D59, Waterborne Urethane Varnish

Where Semi-Gloss finish is required substitute 2nd, 3rd & 4th coats with:

2nd coat:	Resene Aquaclear Semi-Gloss D59, Waterborne Urethane Varnish

3rd coat:	Resene Aquaclear Semi-Gloss D59, Waterborne Urethane Varnish

4th coat:	Resene Aquaclear Semi-Gloss D59, Waterborne Urethane Varnish

Where Solvent-borne Gloss finish is required substitute 2nd, 3rd & 4th coats with:

2nd coat:	Resene Qristal Clear Gloss D52, Solvent-borne Polyurethane Varnish

3rd coat:	Resene Qristal Clear Gloss D52, Solvent-borne Polyurethane Varnish

4th coat:	Resene Qristal Clear Gloss D52, Solvent-borne Polyurethane Varnish

Where Solvent-borne Semi-Gloss finish is required substitute 2nd, 3rd & 4th coats with:

2nd coat:	Resene Qristal Clear Semi-Gloss D52, Solvent-borne Polyurethane

3rd coat:	Resene Qristal Clear Semi-Gloss D52, Solvent-borne Polyurethane

4th coat:	Resene Qristal Clear Semi-Gloss D52, Solvent-borne Polyurethane

Where Solvent-borne Flat finish is required substitute 2nd, 3rd & 4th coats only with:

2nd coat:	Resene Qristal Clear Flat D52, Solvent-borne Polyurethane Varnish

3rd coat:	Resene Qristal Clear Flat D52, Solvent-borne Polyurethane Varnish

4th coat:	Resene Qristal Clear Flat D52, Solvent-borne Polyurethane Varnish

### 4.39	RESENE NEW INTERIOR TIMBER WALLS, CEILINGS - PARTICLE BOARD, MDF, PLYWOOD - WHITEWASH

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 10/1

1st coat:	Resene Colorwood Whitewash D50W, Waterborne Urethane

2nd coat:	Resene Aquaclear Satin D59, Waterborne Urethane Varnish

3rd coat:	Resene Aquaclear Satin D59, Waterborne Urethane Varnish

4th coat:	Resene Aquaclear Satin D59, Waterborne Urethane Varnish

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Gloss finish is required substitute 2nd, 3rd & 4th coats with:

2nd coat:	Resene Aquaclear Gloss D59, Waterborne Urethane Varnish

3rd coat:	Resene Aquaclear Gloss D59, Waterborne Urethane Varnish

4th coat:	Resene Aquaclear Gloss D59, Waterborne Urethane Varnish

Where Semi-Gloss finish is required substitute 2nd, 3rd & 4th coats with:

2nd coat:	Resene Aquaclear Semi-Gloss D59, Waterborne Urethane Varnish

3rd coat:	Resene Aquaclear Semi-Gloss D59, Waterborne Urethane Varnish

4th coat:	Resene Aquaclear Semi-Gloss D59, Waterborne Urethane Varnish

### 4.40	RESENE NEW INTERIOR TIMBER FLOOR - PAINT

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 12/1

1st coat:	Resene Quick Dry D45, Waterborne Acrylic Primer Undercoat

2nd coat:	Resene Walk-On Flooring & Paving Paint D322, Waterborne

3rd coat:	Resene Walk-On Flooring & Paving Paint D322, Waterborne

4th coat:	Resene Concrete Wax D508, Waterborne Satin Glaze

Where an   acrylic   satin   finish is required substitute 2nd, 3rd & 4th coats with  :

2nd coat:	Resene Lumbersider D34, Satin Acrylic

3rd coat:	Resene Lumbersider D34, Satin Acrylic

Where a Semi-Gloss finish is required substitute 2nd,3rd & 4th coats with:

2nd coat:	Resene Lustacryl D310, Waterborne Enamel

3rd coat:	Resene Lustacryl D310, Waterborne Enamel

Where a 2 pack Urethane finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Uracryl 802 RA55W, Water-borne Semi-Gloss Urethane

3rd coat:	Resene Uracryl 802 RA55W, Water-borne Semi-Gloss Urethane

Allow Resene Quick Dry to dry for 24 hours prior to applying Resene Uracryl 802

### 4.41	RESENE NEW INTERIOR TIMBER FLOOR - CLEAR COAT, SINGLE PACK

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 11/1

1st coat:	Resene Qristal ClearFloor 1K D506, Waterborne Flooring Urethane

2nd coat:	Resene Qristal ClearFloor 1K D506, Waterborne Flooring Urethane

3rd coat:	Resene Qristal ClearFloor 1K D506, Waterborne Flooring Urethane

Note: This system should be used for Low/Medium traffic.  For high traffic use 2 pack option.

### 4.42	RESENE NEW INTERIOR TIMBER FLOOR – CLEAR COAT, TWO PACK

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 11/1

1st coat:	Resene Qristal ClearFloor 2K D506a, Waterborne Flooring Urethane

2nd coat:	Resene Qristal ClearFloor 2K D506a, Waterborne Flooring Urethane

3rd coat:	Resene Qristal ClearFloor 2K D506a, Waterborne Flooring Urethane

Note: This system is suitable for high traffic

### 4.43	RESENE NEW INTERIOR TIMBER FLOOR – STAIN

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 11/1

1st coat:	Resene Colorwood D50a, Waterborne Natural Wood stain

2nd coat:	Resene Qristal ClearFloor 1K D506, Waterborne Flooring Urethane

3rd coat:	Resene Qristal ClearFloor 1K D506, Waterborne Flooring Urethane

4th coat:	Resene Qristal ClearFloor 1K D506, Waterborne Flooring Urethane

Note: This system should be used for Low/Medium traffic.

For High traffic areas substitute 2nd, 3rd, 4th coats with 2 pack top coats:

2nd coat:	Resene Qristal ClearFloor 2K D506a, Waterborne Flooring Urethane

3rd coat:	Resene Qristal ClearFloor 2K D506a, Waterborne Flooring Urethane

4th coat:	Resene Qristal ClearFloor 2K D506a, Waterborne Flooring Urethane

### 4.44	RESENE NEW INTERIOR TIMBER FLOOR – PRO-SELECT CLEAR COAT

Professional Flooring Contractor Product

Surface Prep:	Resene SIPDS No6 and Spec Sheet 6: 1/1

1st coat:	Resene ProSelect PS01, 2K Waterborne Flooring Polyurethane

2nd coat:	Resene ProSelect PS01, 2K Waterborne Flooring Polyurethane

3rd coat:	Resene ProSelect PS01, 2K Waterborne Flooring Polyurethane

Note: This system is for use by professional flooring contractors only. Refer to the Resene Pro-Select Data Sheet for all product and technical information.

Interior timber - existing

### 4.45	RESENE EXISTING INTERIOR TIMBER DOORS, JOINERY, SKIRTING

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 9/3

Spot Prime:	Resene Quick Dry D45, Waterborne Acrylic Primer Undercoat

1st coat:	Resene Lustacryl D310, Waterborne Enamel

2nd coat:	Resene Lustacryl D310, Waterborne Enamel

Note: This section assumes the existing coating is enamel (which must be thoroughly abraded)

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a Gloss finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Enamacryl D309, Waterborne Enamel

2nd coat:	Resene Enamacryl D309, Waterborne Enamel

Where a Low sheen finish is required substitute 1st & 2nd coats with:

1st coat:	Resene SpaceCote Low sheen D311, Waterborne Enamel

2nd coat:	Resene SpaceCote Low sheen D311, Waterborne Enamel

Where a Semi-Gloss solvent-borne finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Lusta-Glo D33, solvent-borne Semi-Gloss Enamel (NEC)

2nd coat:	Resene Lusta-Glo D33, solvent-borne Semi-Gloss Enamel (NEC)

Where a Low sheen solvent-borne finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Room Velvet D320, solvent-borne Low Sheen Enamel (NEC)

2nd coat:	Resene Room Velvet D320, solvent-borne Low Sheen Enamel (NEC)

### 4.46	RESENE EXISTING INTERIOR TIMBER DOORS, JOINERY, SKIRTING – CEDAR

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 9/3

Spot Prime:	Resene Enamel Undercoat D44, Solvent-borne Undercoat (NEC)

1st coat:	Resene Lustacryl D310, Waterborne Enamel

2nd coat:	Resene Lustacryl D310, Waterborne Enamel

Note: This section assumes the existing coating is enamel (which must be thoroughly abraded).

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a Gloss finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Enamacryl D309, Waterborne Enamel

2nd coat:	Resene Enamacryl D309, Waterborne Enamel

Where a Low sheen finish is required substitute 1st & 2nd coats with:

1st coat:	Resene SpaceCote Low sheen D311, Waterborne Enamel

2nd coat:	Resene SpaceCote Low sheen D311, Waterborne Enamel

Where a Semi-Gloss solvent-borne finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Lusta-Glo D33, solvent-borne Semi-Gloss (NEC)

2nd coat:	Resene Lusta-Glo D33, solvent-borne Semi-Gloss (NEC)

Where a Low sheen solvent-borne finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Room Velvet D320, solvent-borne Low Sheen Enamel (NEC)

2nd coat:	Resene Room Velvet D320, solvent-borne Low Sheen Enamel (NEC)

### 4.47	RESENE EXISTING INTERIOR TIMBER DOORS, JOINERY, SKIRTING – CLEAR COAT

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 10/3

1st coat:	Resene Aquaclear Satin D59, Waterborne Urethane Varnish

2nd coat::	Resene Aquaclear Satin D59, Waterborne Urethane Varnish

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Gloss finish is required substitute 1st, 2nd coats with:

1st coat:	Resene Aquaclear Gloss D59, Waterborne Urethane Varnish

2nd coat:	Resene Aquaclear Gloss D59, Waterborne Urethane Varnish

Where Semi-Gloss finish is required substitute 1st, 2nd coats with:

1st coat:	Resene Aquaclear Semi-Gloss D59, Waterborne Urethane Varnish

2nd coat:	Resene Aquaclear Semi-Gloss D59, Waterborne Urethane Varnish

Where Solvent-borne Gloss finish is required substitute 1st, 2nd coats with:

1st coat:	Resene Qristal Clear Gloss D52, Solvent-borne Polyurethane (NEC)

2nd coat:	Resene Qristal Clear Gloss D52, Solvent-borne Polyurethane (NEC)

Where Solvent-borne Semi-Gloss finish is required substitute 1st, 2nd coats with:

1st coat:	Resene Qristal Clear Semi-Gloss D52, Solvent-bornePolyurethane(NEC)

2nd coat:	Resene Qristal Clear Semi-Gloss D52, Solvent-bornePolyurethane(NEC)

### 4.48	RESENE EXISTING INTERIOR TIMBER WALLS, CEILINGS - PARTICLE BOARD, MDF, PLYWOOD

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 14/3

Spot Prime:	Resene Quick Dry D45, Waterborne Acrylic Primer Undercoat

1st coat:	Resene Spacecote Low Sheen D311, Waterborne Enamel

2nd coat:	Resene Spacecote Low Sheen D311, Waterborne Enamel

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a Flat finish is required substitute 1st & 2nd coats with:

1st coat:	Resene SpaceCote Flat D314, Waterborne Enamel

2nd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

Where a Semi-Gloss finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Lustacryl D310, Waterborne Enamel

2nd coat:	Resene Lustacryl D310, Waterborne Enamel

Where a standard acrylic finish (dry areas only) is required substitute 1st & 2nd coats with:

1st coat:	Resene Zylone Sheen D302, Low Sheen Acrylic

2nd coat:	Resene Zylone Sheen D302, Low Sheen Acrylic

Where a Low Sheen solvent-borne finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Room Velvet D322, Low Sheen solvent-borne Enamel (NEC)

2nd coat:	Resene Room Velvet D322, Low Sheen solvent-borne Enamel (NEC)

Where a Clinical finish is required substitute 1st & 2nd coats with:

1st coat:	Resene ClinicalCote D318, Satin Acrylic

2nd coat:	Resene ClinicalCote D318, Satin Acrylic

### 4.49	RESENE EXISTING INTERIOR TIMBER WALLS, CEILINGS,PARTICLEBOARD, MDF, PLYWOOD – CLEAR

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 10/3

1st coat:	Resene Aquaclear Satin D59, Waterborne Urethane Varnish

2nd coat:	Resene Aquaclear Satin D59, Waterborne Urethane Varnish

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Gloss finish is required substitute 1st, 2nd coats with:

1st coat:	Resene Aquaclear Gloss D59, Waterborne Urethane Varnish

2nd coat:	Resene Aquaclear Gloss D59, Waterborne Urethane Varnish

Where Semi-Gloss finish is required substitute 1st, 2nd coats with:

1st coat:	Resene Aquaclear Semi-Gloss D59, Waterborne Urethane Varnish

2nd coat:	Resene Aquaclear Semi-Gloss D59, Waterborne Urethane Varnish

Where Solvent-borne Gloss finish is required substitute 1st & 2nd coats only with:

1st coat:	Resene Qristal Clear Gloss D52, Solvent-borne Polyurethane (NEC)

2nd coat:	Resene Qristal Clear Gloss D52, Solvent-borne Polyurethane (NEC)

Where Solvent-borne Semi-Gloss finish is required substitute 1st & 2nd coats only with:

1st coat:	Resene Qristal Clear Semi-Gloss D52, Solvent-bornePolyurethane(NEC)

2nd coat:	Resene Qristal Clear Semi-Gloss D52, Solvent-bornePolyurethane(NEC)

Where Solvent-borne Flat finish is required substitute 1st & 2nd coats only with:

1st coat:	Resene Qristal Clear Flat D52, Solvent-borne Polyurethane (NEC)

2nd coat:	Resene Qristal Clear Flat D52, Solvent-borne Polyurethane (NEC)

### 4.50	RESENE EXISTING INTERIOR TIMBER FLOOR – CLEAR COAT, SINGLE PACK

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 11/3

1st coat:	Resene Qristal ClearFloor 1K D506, Waterborne Flooring Urethane

2nd coat:	Resene Qristal ClearFloor 1K D506, Waterborne Flooring Urethane

3rd coat:	Resene Qristal ClearFloor 1K D506, Waterborne Flooring Urethane

Note: This system should be used for Low/Medium traffic. For high traffic use 2 pack option.

Where extra durability is required add 4th coat:

4th coat	Resene Qristal ClearFloor 1K D506, Waterborne Flooring Urethane

### 4.51	RESENE EXISTING INTERIOR TIMBER FLOOR – CLEAR COAT, TWO PACK

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 11/3

1st coat:	Resene Qristal ClearFloor 2K D506a, Waterborne Flooring Urethane

2nd coat:	Resene Qristal ClearFloor 2K D506a, Waterborne Flooring Urethane

3rd coat:	Resene Qristal ClearFloor 2K D506a, Waterborne Flooring Urethane

Note: This system is suitable for high traffic

Where extra durability is required add 4th coat:

4th coat	Resene Qristal ClearFloor 2K D506a, Waterborne Flooring Urethane

Interior fibre cement - new

### 4.52	RESENE NEW INTERIOR FIBRE CEMENT, WALLS - DRY AREAS

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 6/1

1st coat:	Resene Concrete Primer D405, Acrylic Concrete Primer

2nd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

3rd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Flat finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

3rd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

Where a standard acrylic finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Zylone Sheen D302, Low Sheen Acrylic

3rd coat:	Resene Zylone Sheen D302, Low Sheen Acrylic

Where a solvent-borne finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Room Velvet D302, solvent-borne Low Sheen (NEC)

3rd coat:	Resene Room Velvet D302, solvent-borne Low Sheen (NEC)

### 4.53	RESENE NEW INTERIOR FIBRE CEMENT, WALLS - CLINICAL DRY AREAS

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 6/1

1st coat:	Resene Concrete Primer D405, Acrylic Concrete Primer

2nd coat:	Resene ClinicalCote Satin D318, Waterborne

3rd coat:	Resene ClinicalCote Satin D318, Waterborne

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a Low Sheen finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene ClinicalCote Low Sheen D318, Waterborne

3rd coat:	Resene ClinicalCote Low Sheen D318, Waterborne

For Clinical Walls Wet Areas refer to standard RESENE NEW INTERIOR FIBRE CEMENT, WALLS, WET AREAS clause.

### 4.54	RESENE NEW INTERIOR FIBRE CEMENT, WALLS - WET AREAS

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 6/1

1st coat:	Resene Sureseal D42, Solvent-borne pigmented sealer (NEC)

2nd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

3rd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Flat finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

3rd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

### 4.55	RESENE NEW INTERIOR FIBRE CEMENT, WALLS - CLEAR COAT

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 6/1

1st coat:	Resene Concrete Clear - Gloss D54a, Waterborne Clear

2nd coat:	Resene Concrete Clear - Gloss D54a, Waterborne Clear

3rd coat:	Resene Concrete Clear - Gloss D54a, Waterborne Clear

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Flat finish is required substitute 2nd & 3rd coats only with:

2nd coat:	Resene Concrete Clear - Flat D54a, Waterborne Clear

3rd coat:	Resene Concrete Clear - Flat D54a, Waterborne Clear

Where Satin finish is required substitute 2nd & 3rd coats only with:

2nd coat:	Resene Concrete Clear - Satin D54a, Waterborne Clear

3rd coat:	Resene Concrete Clear - Satin D54a, Waterborne Clear

### 4.56	RESENE NEW INTERIOR FIBRE CEMENT, CEILINGS - DRY AREAS

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 6/1

1st coat:	Resene Concrete Primer D405, Acrylic Concrete Primer

2nd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

3rd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a standard acrylic finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Ceiling Paint D305, Flat Acrylic

3rd coat:	Resene Ceiling Paint D305, Flat Acrylic

### 4.57	RESENE NEW INTERIOR FIBRE CEMENT, CEILINGS - CLINICAL DRY AREAS

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 6/1

1st coat:	Resene Concrete Primer D405, Acrylic Concrete Primer

2nd coat:	Resene ClinicalCote Low-Sheen D318, Waterborne

3rd coat:	Resene ClinicalCote Low-Sheen D318, Waterborne

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a Satin finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene ClinicalCote Satin D318, Waterborne

3rd coat:	Resene ClinicalCote Satin D318, Waterborne

For Clinical Ceilings Wet Areas refer to standard RESENE NEW INTERIOR FIBRE CEMENT, CEILINGS, WET AREAS clause.

### 4.58	RESENE NEW INTERIOR FIBRE CEMENT, CEILINGS - WET AREAS

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 6/1

1st coat:	Resene Sureseal D42, Solvent-borne pigmented sealer (NEC)

2nd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

3rd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Low Sheen is required substitute 2nd & 3rd coats with:

2nd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

3rd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

Where a solvent-borne finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Room Velvet D302, solvent-borne Low Sheen (NEC)

3rd coat:	Resene Room Velvet D302, solvent-borne Low Sheen (NEC)

### 4.59	RESENE NEW INTERIOR FIBRE CEMENT, CEILINGS - CLEAR COAT

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 6/1

1st coat:	Resene Concrete Clear - Gloss D54a, Waterborne Clear

2nd coat:	Resene Concrete Clear - Gloss D54a, Waterborne Clear

3rd coat:	Resene Concrete Clear - Gloss D54a, Waterborne Clear

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Flat finish is required substitute 2nd & 3rd coats only with:

2nd coat:	Resene Concrete Clear - Flat D54a, Waterborne Clear

3rd coat:	Resene Concrete Clear - Flat D54a, Waterborne Clear

Where Satin finish is required substitute 2nd & 3rd coats only with:

2nd coat:	Resene Concrete Clear - Satin D54a, Waterborne Clear

3rd coat:	Resene Concrete Clear - Satin D54a, Waterborne Clear

Interior fibre cement - existing

### 4.60	RESENE EXISTING INTERIOR FIBRE CEMENT, WALLS - DRY AREAS

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 6/3

Spot Prime:	Resene Concrete Primer D405, Acrylic Concrete Primer

2nd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

3rd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Note: Assumes existing coating is acrylic

Where Flat finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

3rd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

Where a standard acrylic finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Zylone Sheen D302, Low Sheen Acrylic

3rd coat:	Resene Zylone Sheen D302, Low Sheen Acrylic

Where a solvent-borne finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Room Velvet D302, solvent-borne Low Sheen (NEC)

3rd coat:	Resene Room Velvet D302, solvent-borne Low Sheen (NEC)

### 4.61	RESENE EXISTING INTERIOR FIBRE CEMENT, WALLS - WET AREAS

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 6/3

Spot Prime:	Resene Sureseal D42, Solvent-borne pigmented sealer (NEC)

2nd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

3rd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Flat finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

3rd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

Where a solvent-borne finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Room Velvet D302, solvent-borne Low Sheen (NEC)

3rd coat:	Resene Room Velvet D302, solvent-borne Low Sheen (NEC)

### 4.62	RESENE EXISTING INTERIOR FIBRE CEMENT, CEILINGS, DRY AREAS

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 6/3

Spot Prime:	Resene Concrete Primer D405, Acrylic Concrete Primer

2nd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

3rd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a standard acrylic finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Ceiling Paint D305, Flat Acrylic

3rd coat:	Resene Ceiling Paint D305, Flat Acrylic

### 4.63	RESENE EXISTING INTERIOR FIBRE CEMENT, CEILINGS - WET AREAS

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 6/3

Spot Prime:	Resene Sureseal D42, Solvent-borne pigmented sealer (NEC)

2nd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

3rd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Low Sheen is required substitute 2nd & 3rd coats with:

2nd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

3rd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

Where a solvent-borne finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Room Velvet D302, solvent-borne Low Sheen (NEC)

3rd coat:	Resene Room Velvet D302, solvent-borne Low Sheen (NEC)

Interior fibrous plaster - new

### 4.64	RESENE NEW INTERIOR FIBROUS PLASTER, WALLS

Surface Prep:	Resene SIPDS No1 and Spec Sheet 1: 6/1

1st coat:	Resene Sureseal D42, Solvent-borne pigmented sealer (NEC)

2nd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

3rd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Flat finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

3rd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

### 4.65	RESENE NEW INTERIOR FIBROUS PLASTER, CEILINGS

Surface Prep:	Resene SIPDS No1 and Spec Sheet 1: 6/1

1st coat:	Resene Sureseal D42, Solvent-borne pigmented sealer (NEC)

2nd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

3rd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a Low Sheen finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

3rd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

Interior fibrous plaster - existing

### 4.66	RESENE EXISTING INTERIOR FIBROUS PLASTER, WALLS

Surface Prep:	Resene SIPDS No1 and Spec Sheet 1: 6/3

Spot Prime:	Resene Sureseal D42, Solvent-borne pigmented sealer (NEC)

2nd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

3rd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

Note: If there is significant staining to the existing coating apply a full coat of Resene Sureseal.

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Flat finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

3rd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

### 4.67	RESENE EXISTING INTERIOR FIBROUS PLASTER, CEILINGS

Surface Prep:	Resene SIPDS No1 and Spec Sheet 1: 6/3

Spot Prime:	Resene Sureseal D42, Solvent-borne pigmented sealer (NEC)

2nd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

3rd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

Note: If there is significant staining to the existing coating apply a full coat of Resene Sureseal.

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a low sheen finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

3rd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

Interior cementitious - new

### 4.68	RESENE NEW INTERIOR INSITU CONCRETE /PRECAST/ BLOCKS, WALLS - DRY AREAS

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 6/1

1st coat:	Resene Concrete Primer D405, Acrylic Concrete Primer

2nd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

3rd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Flat finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

3rd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

Where Semi-Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Lustacryl D310, Waterborne Enamel

3rd coat:	Resene Lustacryl D310, Waterborne Enamel

Where a standard acrylic finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Zylone Sheen D302, Low Sheen Acrylic

3rd coat:	Resene Zylone Sheen D302, Low Sheen Acrylic

Where a 2 pack Urethane finish is required substitute 2nd & 3rd coats coats with:

2nd coat:	Resene Uracryl 802 RA55W, Water-borne Semi-Gloss Urethane (NEC)

3rd coat:	Resene Uracryl 802 RA55W, Water-borne Semi-Gloss Urethane (NEC)

Allow Resene Quick Dry to dry for 24 hours prior to applying Resene Uracryl 802

### 4.69	RESENE NEW INTERIOR INSITU CONCRETE/ PRECAST/ BLOCKS, WALLS - WET AREAS

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 6/1

1st coat:	Resene Sureseal D42, Solvent-borne pigmented sealer (NEC)

2nd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

3rd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Flat finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

3rd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

Where Semi-Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Lustacryl D310, Waterborne Enamel

3rd coat:	Resene Lustacryl D310, Waterborne Enamel

### 4.70	RESENE NEW INTERIOR INSITU CONCRETE/ PRECAST/ BLOCKS, WALLS - CLEAR COAT

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 6/1

1st coat:	Resene Concrete Clear - Gloss D54a, Waterborne Clear

2nd coat:	Resene Concrete Clear - Satin D54a, Waterborne Clear

3rd coat:	Resene Concrete Clear - Satin D54a, Waterborne Clear

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Flat finish is required substitute 2nd & 3rd coats only with:

2nd coat:	Resene Concrete Clear - Flat D54a, Waterborne Clear

3rd coat:	Resene Concrete Clear - Flat D54a, Waterborne Clear

Where Gloss finish is required substitute 2nd & 3rd coats only with:

2nd coat:	Resene Concrete Clear - Gloss D54a, Waterborne Clear

3rd coat:	Resene Concrete Clear - Gloss D54a, Waterborne Clear

### 4.71	RESENE NEW INTERIOR INSITU CONCRETE/ PRECAST/ BLOCKS, CEILINGS - DRY AREAS

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 6/1

1st coat:	Resene Concrete Primer D405, Acrylic Concrete Primer

2nd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

3rd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Low Sheen is required substitute 2nd & 3rd coats with:

2nd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

3rd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

Where Semi-Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Lustacryl D310, Waterborne Enamel

3rd coat:	Resene Lustacryl D310, Waterborne Enamel

Where a standard acrylic finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Ceiling Paint D305, Flat Acrylic

3rd coat:	Resene Ceiling Paint D305, Flat Acrylic

Where a 2 pack Urethane finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Uracryl 802 RA55W, Water-borne Semi-Gloss Urethane (NEC)

3rd coat:	Resene Uracryl 802 RA55W, Water-borne Semi-Gloss Urethane (NEC)

Allow Resene Concrete Primer to dry for 48 hours prior to applying Resene Uracryl 802

### 4.72	RESENE NEW INTERIOR INSITU CONCRETE/ PRECAST/ BLOCKS, CEILINGS - WET AREAS

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 6/1

1st coat:	Resene Sureseal D42, Solvent-borne pigmented sealer (NEC)

2nd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

3rd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Low Sheen is required substitute 2nd & 3rd coats with:

2nd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

3rd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

Where Semi-Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Lustacryl D310, Waterborne Enamel

3rd coat:	Resene Lustacryl D310, Waterborne Enamel

Where a solvent-borne finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Room Velvet D302, solvent-borne Low Sheen (NEC)

3rd coat:	Resene Room Velvet D302, solvent-borne Low Sheen (NEC)

### 4.73	RESENE NEW INTERIOR INSITU CONCRETE/ PRECAST/ BLOCKS, CEILINGS - CLEAR COAT

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 6/1

1st coat:	Resene Concrete Clear - Gloss D54a, Waterborne Clear

2nd coat:	Resene Concrete Clear - Satin D54a, Waterborne Clear

3rd coat:	Resene Concrete Clear - Satin D54a, Waterborne Clear

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Flat finish is required substitute 2nd & 3rd coats only with:

2nd coat:	Resene Concrete Clear - Flat D54a, Waterborne Clear

3rd coat:	Resene Concrete Clear - Flat D54a, Waterborne Clear

Where Gloss finish is required substitute 2nd & 3rd coats only with:

2nd coat:	Resene Concrete Clear - Gloss D54a, Waterborne Clear

3rd coat:	Resene Concrete Clear - Gloss D54a, Waterborne Clear

### 4.74	RESENE NEW INTERIOR CONCRETE FLOOR – PAINT 2 PACK WATERBORNE EPOXY

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 7/1

Sealer coat	Resene ArmourBond - RA408, Clear Epoxy Sealer

1st coat:	Resene Aquapoxy Gloss – RA43, Waterborne Epoxy

2nd coat:	Resene Aquapoxy Gloss – RA43, Waterborne Epoxy

3rd coat:	Resene Aquapoxy Gloss – RA43, Waterborne Epoxy

Note: suitable for Garage Floors

Where a Semi-Gloss finish is required substitute 1st, 2nd, 3rd coats with:

1st coat:	Resene Aquapoxy Semi-Gloss – RA43, Waterborne Epoxy

2nd coat:	Resene Aquapoxy Semi-Gloss – RA43, Waterborne Epoxy

3rd coat:	Resene Aquapoxy Semi-Gloss – RA43, Waterborne Epoxy

Where a “Non-Skid” system is required substitute 2nd coat only with:

2nd coat:	Resene Aquapoxy – RA43, Waterborne Epoxy modified with 2kg of Resene SRG per 4litre mix

### 4.75	RESENE NEW INTERIOR CONCRETE FLOOR – PAINT 2 PACK SOLVENTBORNE EPOXY

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 7/1

Sealer coat::	Resene ArmourBond - RA408, Clear Epoxy Sealer

1st coat:	Resene Armourcote 510 – RA40, 2 Pack High Solids Epoxy

2nd coat:	Resene Armourcote 510 – RA40, 2 Pack High Solids Epoxy

Note: suitable for Commercial Floors

### 4.76	RESENE NEW INTERIOR CONCRETE FLOOR – PAINT SINGLE PACK

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 7/1

1st coat	Resene ConcreteSeal 3in1 – D409, Solvent-borne Sealer

2nd coat:	Resene Walk-On Flooring & Paving Paint – D322, Waterborne

3rd coat:	Resene Walk-On Flooring & Paving Paint – D322, Waterborne

4th coat:	Resene Concrete Wax – D508, Waterborne Satin Glaze

Note: Unsuitable for Garage Floors

Where a "Non-Skid" system is required substitute 2nd coat only with:

2nd coat:	Resene Walk-On Flooring & Paving Paint -; D322, Waterborne modified with 2kg of Resene SRG per 4litre mix

### 4.77	RESENE NEW INTERIOR CONCRETE FLOOR – CLEAR COAT SINGLE PACK

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 7/1

1st coat:	Resene Concrete Wax – D508, Waterborne Satin Glaze

2nd coat:	Resene Concrete Wax – D508, Waterborne Satin Glaze

3rd coat:	Resene Concrete Wax – D508, Waterborne Satin Glaze

4th coat:	Resene Concrete Wax – D508, Waterborne Satin Glaze

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Note: Unsuitable for Garage Floors

### 4.78	RESENE NEW INTERIOR CONCRETE FLOOR – CLEAR COAT TWO PACK

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 7/1

1st coat:	Resene Uracryl 403 Gloss Clear – RA56 (thinned 15%), 2 Pack Urethane

2nd coat:	Resene Uracryl 403 Gloss Clear – RA56, 2 Pack Urethane

3rd coat:	Resene Uracryl 403 Gloss Clear – RA56, 2 Pack Urethane

Note: suitable for Garage Floors

Where a Semi-Gloss finish is required substitute 2nd & 3rd coats only with:

2nd coat:	Resene Uracryl 402 Semi-Gloss Clear – RA55, 2 Pack Urethane

3rd coat:	Resene Uracryl 402 Semi-Gloss Clear – RA55, 2 Pack Urethane

Where a Low Sheen finish is required substitute 2nd & 3rd coats only with:

2nd coat:	Resene Uracryl 404 Low Sheen Clear – RA59, 2 Pack Urethane

3rd coat:	Resene Uracryl 404 Low Sheen Clear – RA59, 2 Pack Urethane

Interior cementitious - existing

### 4.79	RESENE EXISTING INTERIOR INSITU CONCRETE/ PRECAST/ BLOCKS, WALLS - DRY AREAS

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 6/3

Spot Prime:	Resene Concrete Primer D405, Acrylic Concrete Primer

1st coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

2nd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Flat finish is required substitute 1st & 2nd coats with:

1st coat:	Resene SpaceCote Flat D314, Waterborne Enamel

2nd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

Where Semi-Gloss finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Lustacryl D310, Waterborne Enamel

2nd coat:	Resene Lustacryl D310, Waterborne Enamel

Where a standard acrylic finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Zylone Sheen D302, Low Sheen Acrylic

2nd coat:	Resene Zylone Sheen D302, Low Sheen Acrylic

Where a solvent-borne finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Room Velvet D302, Solvent-borne Low Sheen (NEC)

2nd coat:	Resene Room Velvet D302, Solvent-borne Low Sheen (NEC)

### 4.80	RESENE EXISTING INTERIOR INSITU CONCRETE/ PRECAST/ BLOCKS, WALLS - WET AREAS

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 6/3

Spot Prime:	Resene Sureseal D42, Solvent-borne pigmented sealer (NEC)

1st coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

2nd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Flat finish is required substitute 1st & 2nd coats with:

1st coat:	Resene SpaceCote Flat D314, Waterborne Enamel

2nd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

Where Semi-Gloss finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Lustacryl D310, Waterborne Enamel

2nd coat:	Resene Lustacryl D310, Waterborne Enamel

### 4.81	RESENE EXISTING INTERIOR INSITU CONCRETE/ PRECAST/ BLOCKS, CEILINGS - DRY AREAS

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 6/3

Spot Prime:	Resene Concrete Primer D405, Acrylic Concrete Primer

1st coat:	Resene SpaceCote Flat D314, Waterborne Enamel

2nd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Low Sheen is required substitute 1st & 2nd coats with:

1st coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

2nd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

Where Semi-Gloss finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Lustacryl D310, Waterborne Enamel

2nd coat:	Resene Lustacryl D310, Waterborne Enamel

Where a standard acrylic finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Ceiling Paint D305, Flat Acrylic

2nd coat:	Resene Ceiling Paint D305, Flat Acrylic

Where a solvent-borne finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Room Velvet D302, solvent-borne Low Sheen (NEC)

2nd coat:	Resene Room Velvet D302, solvent-borne Low Sheen (NEC)

### 4.82	RESENE EXISTING INTERIOR INSITU CONCRETE/ PRECAST/ BLOCKS, CEILINGS - WET AREAS

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 6/3

Spot Prime:	Resene Sureseal D42, Solvent-borne pigmented sealer (NEC)

1st coat:	Resene SpaceCote Flat D314, Waterborne Enamel

2nd coat:	Resene SpaceCote Flat D314, Waterborne Enamel

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Low Sheen is required substitute 1st & 2nd coats with:

1st coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

2nd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

Where Semi-Gloss finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Lustacryl D310, Waterborne Enamel

2nd coat:	Resene Lustacryl D310, Waterborne Enamel

Where a solvent-borne finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Room Velvet D302, solvent-borne Low Sheen (NEC)

2nd coat:	Resene Room Velvet D302, solvent-borne Low Sheen (NEC)

### 4.83	RESENE EXISTING INTERIOR CONCRETE FLOOR – PAINT 2 PACK WATERBORNE EPOXY

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 7/3

Spot Prime:	Resene ArmourBond - RA408, Clear Epoxy Sealer

1st coat:	Resene Aquapoxy Gloss – RA43, Waterborne Epoxy

2nd coat:	Resene Aquapoxy Gloss – RA43, Waterborne Epoxy

Note: suitable for garage floors.  Assumes existing coating is a 2 pack Epoxy/Urethane

Where a Semi-Gloss finish is required substitute 1st & 2ndcoats with:

1st coat:	Resene Aquapoxy Semi-Gloss – RA42, Waterborne Epoxy

2nd coat:	Resene Aquapoxy Semi-Gloss – RA42, Waterborne Epoxy

### 4.84	RESENE EXISTING INTERIOR CONCRETE FLOOR – PAINT 2 PACK SOLVENTBORNE EPOXY

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 7/3

Spot Prime:	Resene ArmourBond - RA408, Clear Epoxy Sealer

1st coat:	Resene Armourcote 510 – RA40, 2 Pack High Solids Epoxy

2nd coat:	Resene Armourcote 510 – RA40, 2 Pack High Solids Epoxy

Note: suitable for commercial floors.  Assumes existing coating is a 2 pack Epoxy/Urethane.

### 4.85	RESENE EXISTING INTERIOR CONCRETE FLOOR – CLEAR COAT TWO PACK

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 7/3

Spot Prime:	Resene Uracryl 403 Gloss Clear – RA56 (thinned 15%), 2 Pack Urethane

1st coat:	Resene Uracryl 403 Gloss Clear – RA56, 2 Pack Urethane

2nd coat:	Resene Uracryl 403 Gloss Clear – RA56, 2 Pack Urethane

Note: suitable for Garage Floors

Where a Semi-Gloss finish is required substitute 1st & 2nd coats only with:

1st coat:	Resene Uracryl 402 Semi-Gloss Clear – RA55, 2 Pack Urethane

2nd coat:	Resene Uracryl 402 Semi-Gloss Clear – RA55, 2 Pack Urethane

Where a Low Sheen finish is required substitute 1st & 2nd coats only with:

1st coat:	Resene Uracryl 404 Low Sheen Clear – RA59, 2 Pack Urethane

2nd coat:	Resene Uracryl 404 Low Sheen Clear – RA59, 2 Pack Urethane

Interior metal - new

### 4.86	RESENE NEW INTERIOR MILD STEEL

Surface Prep:	Resene SIPDS No4 and Spec Sheet 4: 5/1

1st coat:	Resene GP Metal Primer D411, General Purpose Modified Alkyd (NEC)

2nd coat:	Resene Lustacryl D310, Semi-Gloss Waterborne Enamel

3rd coat:	Resene Lustacryl D310, Semi-Gloss Waterborne Enamel

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Enamacryl D309, Gloss Waterborne Enamel

3rd coat:	Resene Enamacryl D309, Gloss Waterborne Enamel

Where a Low Sheen finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

3rd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

Where a Low Sheen solvent-borne finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Room Velvet D302, Solvent-borne Low Sheen (NEC)

3rd coat:	Resene Room Velvet D302, Solvent-borne Low Sheen (NEC)

Where a Semi-Gloss solvent-borne finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Lusta-Glo D33, Solvent-borne Semi-Gloss (NEC)

3rd coat:	Resene Lusta-Glo D33, Solvent-borne Semi-Gloss (NEC)

For Resene High Performance 2 pack type systems refer to MasterSpec 6745R

### 4.87	RESENE NEW INTERIOR GALVANIZED STEEL

Surface Prep:	Resene SIPDS No4 and Spec Sheet 4: 6/1

1st coat:	Resene Galvo Prime D402, Waterborne Galvanised steel primer (NEC)

2nd coat:	Resene Lustacryl D310, Semi-Gloss Waterborne Enamel

3rd coat:	Resene Lustacryl D310, Semi-Gloss Waterborne Enamel

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Enamacryl D309, Gloss Waterborne Enamel

3rd coat:	Resene Enamacryl D309, Gloss Waterborne Enamel

Where a Low Sheen finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

3rd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

For Resene High Performance 2 pack type systems refer to MasterSpec 6745R

### 4.88	RESENE NEW INTERIOR ALUMINIUM

Surface Prep:	Resene SIPDS No4 and Spec Sheet 4: 8/1

1st coat:	Resene Galvo Prime D402, Waterborne Galvanised steel primer (NEC)

2nd coat:	Resene Lustacryl D310, Semi-Gloss Waterborne Enamel

3rd coat:	Resene Lustacryl D310, Semi-Gloss Waterborne Enamel

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Enamacryl D309, Gloss Waterborne Enamel

3rd coat:	Resene Enamacryl D309, Gloss Waterborne Enamel

For Resene High Performance 2 pack type systems refer to MasterSpec 6745R

Interior metal - existing

### 4.89	RESENE EXISTING INTERIOR MILD STEEL

Surface Prep:	Resene SIPDS No4 and Spec Sheet 4: 5/3

Spot Prime:	Resene GP Metal Primer D411, General Purpose Modified Alkyd (NEC)

1st coat:	Resene Lustacryl D310, Semi-Gloss Waterborne Enamel

2nd coat:	Resene Lustacryl D310, Semi-Gloss Waterborne Enamel

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a Gloss finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Enamacryl D309, Gloss Waterborne Enamel

2nd coat:	Resene Enamacryl D309, Gloss Waterborne Enamel

Where a Low Sheen finish is required substitute 1st & 2nd coats with:

1st coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

2nd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

Where a Low Sheen solvent-borne finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Room Velvet D302, Solvent-borne Low Sheen (NEC)

2nd coat:	Resene Room Velvet D302, Solvent-borne Low Sheen (NEC)

Where a Semi-Gloss solvent-borne finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Lusta-Glo D33, Solvent-borne Semi-Gloss (NEC)

2nd coat:	Resene Lusta-Glo D33, Solvent-borne Semi-Gloss (NEC)

### 4.90	RESENE EXISTING INTERIOR GALVANIZED STEEL

Surface Prep:	Resene SIPDS No4 and Spec Sheet 4: 5/3

Spot Prime:	Resene GP Metal Primer D411, General Purpose Modified Alkyd (NEC)

1st coat:	Resene Lustacryl D310, Semi-Gloss Waterborne Enamel

2nd coat:	Resene Lustacryl D310, Semi-Gloss Waterborne Enamel

Where a Gloss finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Enamacryl D309, Gloss Waterborne Enamel

2nd coat:	Resene Enamacryl D309, Gloss Waterborne Enamel

Where a Low Sheen finish is required substitute 1st & 2nd coats with:

1st coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

2nd coat:	Resene SpaceCote Low Sheen D311, Waterborne Enamel

Where a Low Sheen solvent-borne finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Room Velvet D302, Solvent-borne Low Sheen (NEC)

2nd coat:	Resene Room Velvet D302, Solvent-borne Low Sheen (NEC)

Where a Semi-Gloss solvent-borne finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Lusta-Glo D33, Solvent-borne Semi-Gloss (NEC)

2nd coat:	Resene Lusta-Glo D33, Solvent-borne Semi-Gloss (NEC)